Growth and Optical studies on Glycine Sodium Nitrate by Unidirectional Growth method

J. Mary Linet, S. Jerome Das*

Department of Physics, LoyolaCollege, Nungambakkam, Chennai600034

Corresponding author: Email: sjeromedas2004@yahoo.com

Optically transparent bulk semi-organic single crystals of glycine sodium nitrate have been grown by unidirectional method. The grown crystal was identified using single crystal XRD analysis. The functional groups present in the crystal were confirmed using FTIR analysis. Optical absorption studies reveal very low absorption in the entire visible region, which reveals the good optical quality of the grown crystal. The mechanical properties of the grown crystal were studied using Vickers microhardness tester. Dielectric behaviour of the grown crystal was studied and the results are discussed in detail.