Unidirectional growth of potassium dihydrogen phosphate (KDP) single crystals by modified Sankaranarayanan–Ramasamy (mSR) method

R. Robert1 and   S. Jerome Das 2*

1Department of Physics, Govt. Arts College (Men), Krishnagiri, India

2Department of Physics, Loyola College, Chennai-600 034, India

*Corresponding Author: sjeromedas2004@yahoo.com, jerome@loyolacollege.edu. 	   			    Tel: +9144 2817 5662; fax: +9144 2817 5566

Transparent single crystals of potassium dihydrogen phosphate (KDP) were grown by modified Sankaranarayanan–Ramasamy (SR) method. The band gap energy for the KDP crystals was calculated from optical transmission spectrum. The theoretical calculations to determine the optical constants of the material and a technique for photonic band gap tuning, which is essentially required to develop the optoelectronic devices, were determined using the optical studies. Further, theVicker’s microhardness as well as parameters such as fracture toughness(Kc), brittleness index(B) and yield strength(sv) are presented.